Continuous Bituminous Pavement Stripping

Assessment through Non-Destructive Testing

Task 1 Obtain Data From Pavement Sections Exhibiting Stripping

Task 1 Report

September 30, 2025

A key part of developing a robust method for detection of stripping is to assemble a well-documented data set with adequate independent ground truth to confirm the presence or absence of stripping. While it is understood that data collected specifically for this project will be carried out by the TPF-5(504) and member states, the goal of this task has been to work with the TPF members to ensure that the best available data set is generated.  The following summarizes the data collection process, the data that was obtained, how it was reviewed, and what criteria were used to determine application to the project objectives.

Task 1a. Review existing data on sites with documented stripping

Infrasense obtained access to TSD, 3DGPR, and core data from 24 sites in 10 different states.  A list of these data sources is provided in Table 1. The table shows the state source, the road ID, the available evidence of stripping, and the various types of data available. All data referenced in this table has been received and reviewed to determine the suitability to be used as a basis for development of a stripping evaluation algorithm. Based on this review, a subset of 10 roads from 6 different agencies incorporating data from 160 core locations has been selected for further review and analysis. These have been selected based on clear evidence of stripping and the availability of GPR and deflection data. These selected sections are highlighted in blue in Table 1.

Note that even amongst the sections that have been selected, there is missing data. For example, no surface distress data has been obtained from the KY and MN sites. Such data is usually collected by state highway agencies, and an effort will be made to obtain this missing data.

Task 1b. Recommend a Data Collection Plan

The objective of this subtask is to work with the TPF-5(504) staff to develop a data collection plan that will provide data to support the objectives of this work. The plan has focused on data collection at the MnROAD stripping test section, and was initially intended to address specific test sections where data would be collected specifically for the purposes of this project

    - MnROAD Stripping Test Section

The TPF project constructed a segment at MnROAD with embedded defects to represent stripping. Two types of defects were created – one with coarse rap and one with the original material treated to remove the binder. The layout of test cells is described in Table 2.   Data was collected on this test segment using the following equipment

        - Kontur 3DGPR system collected on 7/31/24 by MnDOT – 3 lines of data (left, right, and center) were collected after the placement of each lift. Each line extended the full length of the test segment, with a sample rate of 17.9 mm per scan

        - PSPA system to collect SASW and Impact Echo data – data was initially collected on 10/28/24 by Infrasense at 1-foot spacing along the centerline of the test segment over about 60% of the length of the segment. Subsequently, MnDOT personnel collected data on 3/24/25 over the entire length of the test section at 1-foot intervals

        - FWD Data – this data was collected by MnDOT personnel on 10/16/2024 at 1-foot intervals along the centerline of the test section

        - TSD Data – This data was collected by ARRB during the week of 8.18.25. That data has not yet been delivered.

Table 1 – Data Sources Provided

Note – sections highlighted in blue were selected for final analysis

| Cell | Length | Description | Features |  |
| --- | --- | --- | --- | --- |
| 2422 | 30 | Control | metal plates at base of lift 1 |  |
| 2421 | 40 | AC over old AC | stripping elements 2-4" deep |  |
| 2420 | 40 | AC over old AC | stripping elements 2-4" deep |  |
| 2419 | 40 | AC over old AC | stripping elements 2-4" deep |  |
| 2418 | 40 | AC over old AC | Stripping elements 4-6" deep |  |
| 2417 | 40 | AC over old AC | Stripping elements 4-6" deep | Water pipes |
| Transition | 20 | AC over old AC and PCC | Millings 4-6” deep | metal plates at base of lift 1 |
| 2416 | 20 | AC over PCC | Stripping elements 4-6" deep | Water pipes |
| 2415 | 20 | AC over PCC | Stripping elements 4-6" deep |  |
| 2414 | 20 | AC over PCC | stripping elements 2-4" deep |  |
| 2413 | 20 | AC over PCC | stripping elements 2-4" deep |  |
| 2412 | 20 | AC over PCC | stripping elements 2-4" deep |  |
| 2411 | 25 | Control | Metal plates at base of lift 1 |  |

Table 2 – Layout of MnROAD Stripping Test Section

ii	Project-specific data collection

At this point we have decided to work with the data sets described above as input into the  Task 2 data analysis task and for the development of specifications for a stripping detection algorithm (Task 3) and associated software (Task 4). Once these steps are complete, recommendations will be made for testing and evaluation, and specific data collection plans will be developed for that purpose.