‘Performance of Recycled Asphalt Shingles (RAS) in Hot Mix Asphalt’

National Pooled Fund Study TPF-5(213)

R. Christopher Williams

Iowa State University

July 15, 2012

During the eleventh quarter, April 1, 2012 through June 30, 2012, the TPF-5(213) team achieved the following components on the project:

- ISU completed testing of dynamic modulus samples for Illinois, Colorado and Wisconsin.

- ISU completed beam fatigue laboratory testing for Illinois, Colorado and Wisconsin mixes.

- MnDOT completed the binder extractions Illinois, Colorado and Wisconsin mixes.

- MnDOT completed DSR testing on Illinois, Colorado and Wisconsin recovered binders.

- Recovered binders and aggregates were delivered to ISU for testing.

- Updates completed on the TPF-5(213) website.

- Next steps for the study include:

- Completion of Minnesota University Semi-circular bend testing for all state demonstration projects;

- Completion of ISU laboratory PG binder testing for Illinois, Colorado and Wisconsin recovered binders;

- Completion of ISU laboratory testing of aggregate gradations for Illinois, Colorado and Wisconsin materials;

- Updates to the TPF-5(213) website;

- Completion and Delivery of HMA-BBR samples to Missouri DOT; and

- Completion of the Draft executive summaries for Iowa, Indiana, Minnesota, and Missouri state demonstration projects for the final report.